Stretchable spring-sheathed yarn sensor for 3D dynamic body reconstruction assisted by transfer learning

Ronghui Wu*, Liyun Ma, Zhiyong Chen, Yating Shi, Yifang Shi, Sai Liu, Xiaowei Chen, Aniruddha Patil, Zaifu Lin, Yifan Zhang, Chuan Zhang, Rui Yu, Changyong Wang, Jin Zhou, Shihui Guo, Weidong Yu*, Xiang Yang Liu*

Dr. R. Wu, Dr.L.Ma, Dr.Z. Chen, Y. Shi, Y. Shi, X. Chen, Dr. A. Patil, Dr.Z. Lin, Prof. S. Guo, Dr. R. Yu, Prof. W. Yu, Prof. X. Y. Liu

College of Ocean and Earth Sciences, State Key Laboratory of Marine Environmental Science, College of Physical Science and Technology, School of Informatics, Xiamen University, Xiamen 361005, China

E-mail: liuxy@xmu.edu.cn

Dr. R. Wu

Prizker School of Molecular Engineering, The University of Chicago, Chicago, 60637, USA.

E-mail: ronghuiwu@uchicago.edu

Dr. R. Wu, Dr.L. Ma, Dr. Y. Zhang, Prof. W. Yu

Key Laboratory of Textile Science &Technology, Ministry of Education, College of Textiles, Donghua University, Shanghai2 01620, China.

E-mail: wdyu@dhu.edu.cn

Dr. S. Liu

College of Textile Science and Engineering (International Institute of Silk), Zhejiang Sci-Tech University, Hangzhou 310018, China

C. Zhang

Chongqing Academy of Metrology and Quality Inspection, Chongqing, 400020, China

Dr. Changyong Wang, Dr. Jin Zhou

Beijing Institute of Basic Medical Sciences, Beijing, 100850, China

Figure S1. Schematic illustration of the implementation process of human body capture and reconstruction for advanced clothing customization. (a) Image of the volunteer wearing smart cloth embedded with SSYS. (b) Schematic illustration of SSYS measuring body dimensions, including waist, chest, shoulder, elbow, and wrist circumferences. (c) Schematic illustration for SSYS measuring human body joint motions. (d) Target domain collected from the real world by the smart cloth. (e) Schematic illustration of the virtual modules. (f) Source domain from the virtual models. (g) Schematic illustration of the TL that combining the target domains and source domains together. (h) Reconstructed dynamic 3D human according to the measured body dimensions and long-time activity tracking. (i) Garment pattern for advanced clothing customization. (j) Virtual fitting effect of the shirt. (k) Comparison of the fitting effect of the virtual with the actual fitting based on the measured circumferences by SSYS.

Figure S2. Schematic diagram of self-made wrapping spinning device.

Figure S3. Modulus-strain curves for SSYS with different twists.

Figure S4. Microscopic pictures of composite yarns with different twists (twist/10cm).

Figure S5. Resistance variation for SSYS with different twists in the strain range of 0%-40%.

Figure S6. Schematic diagram of entangled yarn less than critical contact twist. (a) helix structure schematic diagram; (b) schematic diagram of unfolding helix structure; (c) schematic diagram of wrapped yarn; (d) resistance unit model for wrapped yarn less than critical contact twist; (e) equivalent resistance schematic diagram.

Figure S7. Schematic diagram of entangled yarn at critical contact twist. (a) schematic diagram of helix structure; (b) resistance unit model for wrapped yarn at critical contact twist;(c) schematic diagram of wrapped yarn; (d) equivalent resistance schematic diagram.

Figure S8. Tensile strain sensor for high twist composite yarn. (a) images of high twist composite yarn during stretching from 0% to 100%; (b) SEM images of composite yarn in initial state and at (c) 100% tensile strain; (d) schematic diagram of high twist composite yarn similar to the cylindrical helical spring structure; (e) Stacking between helical coils.

Figure S9. The resistance variation of the SSYSs with different twists in the strain range of 0%-5%.

Figure S10. Resistance variation and fitting curve of sensitive yarns with different lengths.

Figure S11. Resistance variation of SSYS with different twists when bending into different curvature radius.

Figure S12. Human action monitoring of the strain sensor for moving body capture and reconstruction. (a) Optical images and corresponding resistance variation of a yarn sensor attached on the skin of a bent finger at different angles. (b,c) Optical images and continuous resistance variation of a yarn sensor attached on the skin of a bent wrist(b) and elbow(c). (d) Optical images and corresponding resistance variation of a yarn sensor attached on the skin of a bent knee when jumping or walking. (e) Overview of sensing locations of human body monitored by yarn strain sensor. (f) Resistance variation when strain sensor was attached on the human face for facial expression monitoring. (g)Signal detection under various ﬁnger gestures when strain sensor was fixed in the five fingers. (h) The tension sensor is fixed to the throat and acts as a speech recognition sensor to monitor the pronunciation of different syllables.

Figure S13. The mapping from the resistance value to the measured voltage (Vadc_in) of the connected sensor.

Figure S14. The value of loss functions when training the network model for posture prediction. The red and blue curves indicate the values on training and testing dataset respectively.

Figure S15. Schematics of the network model for transfer learning

Figure S16. The pictures of actual shirt fitting effect for two volunteers from different views.

Table S1.  Performance comparison between reported core-shell structure yarn sensors and this work

| Research work | Gauge factor within 0%-5% | Cyclability | Response time | Washability | Ref |
| --- | --- | --- | --- | --- | --- |
| Spandex/CNT/cotton yarn | 0-3.43 | >150 | - | Yes | [1] |
| Graphene/PVA fiber | ~5.02 | >200 | - | - | [2] |
| Nylon-covered rubber/graphene yarn | ~5 | - | - | - | [3] |
| Elastomer-wrapped CNT fiber | <4 | >40000 | < 300 ms | Yes | [4] |
| Graphite nanoplates/PU covered rubber yarn | ~15 | >1000 | - | - | [5] |
| TPU/CNT/Ppy fiber | ~12 | >500 | - | - | [6] |
| Graphene/PVA/ PU yarn | 18-90 | >100 | - | - | [7] |
| Graphite/Silk Fiber | 14.5 | >3000 | ~135 ms | - | [8] |
| Polyurethane/Cotton/CNT | 0.65 | >270000 | - | - | [9] |
| CNT/PVA coated yarn | 2.36 | - | - | - | [10] |
| MXene/PU/PET core-sheath yarn | 0.67 | >100000 | 120ms | - | [11] |
| Carbon ink/elastic core-spun yarn | 6.1 | >1000 | 110 ms | - | [12] |
| CNT/PDMS/polyester yarn | 2.24 | >20 | - | - | [13] |
| RGO/TPU electrospun mat | ~11 | >6000 | 200 ms | - | [14] |
| PU/PE/Graphene yarn | 7~10 | >10,000 | <100 ms | - | [15] |
| Ionic liquids/PDMS based yarn | 1.5-2 | >10,000 | 80 ms | - | [16] |
| Braided yarn/CNT/PU yarn | 46.4 | >1000 | ~ 200ms | Yes | [17] |
| SSYS | 18-65 | >18000 | 12 ms | Yes | This work |

Note: - represents “Note given”.

Table S2. Body circumference values and measurement errors measured by traditional rulers and predicted values from SSYSs with and without transfer learning.

| User | Values | Waist | Chest | Shoulder | Elbow | Wrist |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Actual /mm | 708 | 825 | 995 | 250 | 176 |
|  | Predicted without TL/mm | 652 | 780 | 968 | 265 | 177 |
|  | Error without TL /% | 7.91 | 5.51 | 2.67 | 6.12 | 0.49 |
|  | Predicted with TL /mm | 718 | 847 | 983 | 243 | 174 |
|  | Error with TL /% | 1.42 | 2.71 | 1.19 | 2.63 | 1.01 |
| 2 | Actual /mm | 824 | 927 | 1022 | 255 | 164 |
|  | Predicted without TL/mm | 833 | 932 | 986 | 261 | 155 |
|  | Error without TL /% | 1.11 | 0.49 | 3.49 | 2.37 | 5.22 |
|  | Predicted with TL /mm | 831 | 939 | 1057 | 255 | 168 |
|  | Error with TL /% | 0.88 | 1.25 | 3.42 | 0.19 | 2.42 |
| 3 | Actual /mm | 801 | 880 | 1042 | 227 | 155 |
|  | Predicted without TL/mm | 780 | 866 | 1002 | 226 | 153 |
|  | Error without TL /% | 2.65 | 1.62 | 3.83 | 0.50 | 1.33 |
|  | Predicted with TL /mm | 797 | 881 | 1047 | 223 | 160 |
|  | Error with TL /% | 0.46 | 0.06 | 0.43 | 1.60 | 3.40 |
| 4 | Actual /mm | 948 | 1047 | 1119 | 270 | 165 |
|  | Predicted without TL/mm | 967 | 976 | 1099 | 272 | 160 |
|  | Error without TL /% | 2.01 | 6.80 | 1.76 | 0.74 | 3.03 |
|  | Predicted with TL /mm | 918 | 1059 | 1163 | 264 | 161 |
|  | Error with TL /% | 3.21 | 1.12 | 3.90 | 2.27 | 2.21 |
| 5 | Actual /mm | 775 | 920 | 1063 | 250 | 172 |
|  | Predicted without TL/mm | 728 | 929 | 983 | 265 | 164 |
|  | Error without TL /% | 6.12 | 1.02 | 7.49 | 5.90 | 4.88 |
|  | Predicted with TL /mm | 794 | 939 | 1071 | 241 | 173 |
|  | Error with TL /% | 2.41 | 2.01 | 0.75 | 3.51 | 0.67 |
| 6 | Actual /mm | 780 | 885 | 1026 | 244 | 163 |
|  | Predicted without TL/mm | 738 | 834 | 957 | 253 | 155 |
|  | Error without TL /% | 5.33 | 5.75 | 6.76 | 3.61 | 4.72 |
|  | Predicted with TL /mm | 773 | 873 | 1052 | 237 | 161 |
|  | Error with TL /% | 0.89 | 1.38 | 2.54 | 2.68 | 1.15 |

Reference

[1]	Z. Zeng, B. Hao, D. Li, D. Cheng, G. Cai, X. Wang, Composites Part A: Applied Science and Manufacturing 2021, 149, 106520.

[2]	X. Wang, Y. Qiu, W. Cao, P. Hu, Chemistry of Materials 2015, 27, 6969.

[3]	J. J. Park, W. J. Hyun, S. C. Mun, Y. T. Park, O. O. Park, ACS applied materials & interfaces 2015, 7, 6317.

[4]	Z. Tang, S. Jia, F. Wang, C. Bian, Y. Chen, Y. Wang, B. Li, ACS applied materials & interfaces 2018, 10, 6624.

[5]	J. Wu, Z. Ma, Z. Hao, J. T. Zhang, P. Sun, M. Zhang, Y. Liu, Y. Cheng, Y. Li, B. Zhong, ACS Applied Nano Materials 2019, 2, 750.

[6]	L. Li, P. Shi, L. Hua, J. An, Y. Gong, R. Chen, C. Yu, W. Hua, F. Xiu, J. Zhou, Nanoscale 2018, 10, 118.

[7]	X. Li, T. Hua, B. Xu, Carbon 2017, 118, 686.

[8]	M. Zhang, C. Wang, Q. Wang, M. Jian, Y. Zhang, ACS applied materials & interfaces 2016, 8, 20894.

[9]	Z. Wang, Y. Huang, J. Sun, Y. Huang, H. Hu, R. Jiang, W. Gai, G. Li, C. Zhi, ACS applied materials & interfaces 2016, 8, 24837.

[10]	W. Li, F. Xu, W. Liu, Y. Gao, K. Zhang, X. Zhang, Y. Qiu, Composites Part A: Applied Science and Manufacturing 2018, 108, 107.

[11]	L. Wang, M. Tian, Y. Zhang, F. Sun, X. Qi, Y. Liu, L. Qu, Journal of Materials Science 2020, 55, 6187.

[12]	Z. Duan, Y. Jiang, S. Wang, Z. Yuan, Q. Zhao, G. Xie, X. Du, H. Tai, ACS Sustainable Chemistry & Engineering 2019, 7, 17474.

[13]	J. Wu, Z. Wang, W. Liu, L. Wang, F. Xu, ACS applied materials & interfaces 2019, 11, 44735.

[14]	Y. Wang, J. Hao, Z. Huang, G. Zheng, K. Dai, C. Liu, C. Shen, Carbon 2018, 126, 360.

[15]	Y. Cheng, R. Wang, J. Sun, L. Gao, Advanced materials 2015, 27, 7365.

[16]	S. Chen, H. Liu, S. Liu, P. Wang, S. Zeng, L. Sun, L. Liu, ACS applied materials & interfaces 2018, 10, 4305.

[17]	J. Pan, B. Hao, W. Song, S. Chen, D. Li, L. Luo, Z. Xia, D. Cheng, A. Xu, G. Cai, Composites Part B: Engineering 2020, 183, 107683.