SUPPORTING INFORMATION FOR

Sulfated GAG Mimetic Peptide Nanofibers Enhance Chondrogenic Differentiation of Mesenchymal Stem Cells in Three-Dimensional In Vitro Models

FIGURE S 1. Reverse-HPLC chromatogram and Liquid chromatography-mass spectrometry (LC-MS) analyses of E-PA (a), SO3-PA (b) and K-PA(c).

FIGURE S 2 Scanning electron microscope micrograph of indicated nanofibers.

Table S 1 Sequences, molecular weights and net charges and HPLC Analysis of the peptide amphiphile molecules at pH 7

| PA molecule | PA sequence | Molecular weight (g/mol) | Net Charge (pH7) | Retention Time (min) | Purity (area %) |
| --- | --- | --- | --- | --- | --- |
| SO3-PA | C12-VVAGEGD(K-pbs)S | 1226 | -3 | 10.8 | 97.1 |
| E-PA | C12-VVAGE | 655,82 | -2 | 12.7 | 96.4 |
| K-PA | C12-VVAGK | 654 | +1 | 15.4 | 96.8 |

Table S 2 Composition and net loads of the nanofiber scaffolds

| PA combination | Volume ratio | Net Charge (pH7) |
| --- | --- | --- |
| SO3/K(0); SO3-PA/K-PA | 1:3 | Neutral |
| SO3/K(-); SO3-PA/K-PA | 1:2 | Negative |
| E/K(0); E-PA/K-PA | 1:1 | Neutral |
| E/K(-); E-PA/K-PA | 2:1 | Negative |

Table S 3 Different media and their contents when culturing msenchymal stem cells on peptide nanofibers

| Maintenance medium | 10% FBS + DMEM |
| --- | --- |
| Basal medium | 10-7M Dexamethazone, 1 µM, Transferrin, 6 μg/mL insulin, 3x10-5 M Sodium Selenite, 0.5mg/mL BSA+ DMEM |
| Chondrogenic medium 1 | 10-7M Dexamethazone, 1 µM, Transferin, 6 μg/mL insulin, 3x10-5 M Sodium Selenite, 0.5 mg/mL BSA+ DMEM + 2 ng/mL TGF beta-1 |
| Chondrogenic medium 2 | 10-7M Deksamethazone, 1 µM, Transferin, 6 μg/mL Insulin, 3x10-5 M Sodium Selenite, 0.5 mg/mL BSA+ DMEM + 10 ng/mL TGF beta-1 |

FIGURE S 3 Representative images of adhered live mouse mesenchmal stem cells at (a) 1 h and (b) 3 h of culture on various coatings (1; E/K (0), 2;E/K (-), 3;SO3/K (0), 4;SO3/K (-), 5;TCP and 6; Collagen I. Live cells stained with Calcein AM (green).

FIGURE S 4 Light microscope images of mouse mesenchymal stem cells cultured on (a) E/K (0), E/K (-) and (b) SO3/K(0), SO3/K(-) coatings in 1; maintenance medium, 2; basal medium, 3; chondrogenic medium 1 and 4; chondrogenic medium at day 7.

FIGURE S 5 Mouse mesenchymal stem cells cultured on E/K (-) and SO3/K (-) coatings express cartilage specific Aggrecan proteins on day 7. Collagen II were labeled with Cy3 secondary antibody (green) and cell nuclei were labeled with DAPI®-3 (blue).

FIGURE S 6 (a, c) Collagen II (b, d) Aggrecan expression of mouse mesenchymal stem cells on indicated coatings (a, b) on day 7 and (c, d) on day 14 in maintenance, basal, chondrogenic medium 1 and 2. The expression level of each gene was normalized against uncoated tissue culture plate samples (TCP) and GAPDH was used as the internal control. Values represent mean ± SEM, n = 3 (***p < 0.0001, **p < 0.01, *p < 0.05).

e.

f.

FIGURE S 7 (a) 3D culture formation by mixing peptide amphiphiles in a well of 24-well plate. (b) Light microscope images of seeded mouse mesenchymal stem cells in 3-dimensional hydrogels. Images of 3-dimensional hydrogel on day 3 (c) and on day 7 (d) Storage and loss modulus of E/K(-) and SO3(-)  hydrogels  in water (e) and HEPES buffer (f) at pH 7.

FIGURE S 8 (a) Light microscope images of mMSCs cultured in E/K(0) and SO3(0) hydrogels on day 14. (b) Hematoxylin and eosin stainings showing aggregate formation by mMSCs cultured in 3D E/K(0) and SO3(0) hydrogels on day 14. (c) Safranin-O stainings showing glycosaminoglycan depositions by mMSCs cultured in E/K(0) and SO3(0) hydrogels on day 14.

FIGURE S 9 Immunofluorescence collagen II staining on sections of mMSC cultured in 3D E/K(0) and SO3(0) hydrogels on day 14. Collagen II were labeled with Cy3 secondary antibody (green) and cell nuclei were labeled with DAPI®-3 (blue).

FIGURE S 10 Safranin-O stainings of mouse mesenchymal stem cells cultured in 3-dimensional E/K(-) and SO3(-) hydrogels on day 14 incubated with and without chondroitinase before Safranin-O staining.